PAGE  
[image: image8.png]


[image: image9.png]



[image: image10.jpg]



a d e s i v i

TECHNICAL 

INFORMATION
Review 002 of 01/2012                                     
 Page 3 of 3

	PRODUCT

	JOLLY – MASTIC FOR MARBLE

	FEATURES

	JOLLY – MASTIC FOR MARBLE is formulated with combined synthetic resins. It is mainly used for gluing and filling all types of marbles and natural stones. It has strong adhesive properties, becomes hard and perfectly polishable after drying time. 

The three versions available TIXO, SEMISOLID and LIQUID which facilitate application (see also the brand new semisolid soft) and fast drying properties (the high-speed version is available for the liquid density) quicken production lines.

The liquid and semisolid versions are perfect for normal applications whereas the tixo density is suitable for vertical applications.

	TECHNICAL DATA

	
	TIXO
	SEMISOLID
	LIQUID

	Specific weight (MI 001)
	1800 ± 100 g/l
	1750 ± 50 g/l
	1750 ± 50 g/l

	V.O.C.  (ASTM 2369)
	58 ± 2 g/l
	60 ± 2 g/l
	65 ± 2 g/l

	Viscosity (MI 002)
	1500 ± 100 Pas (T = 25 °C)
	1100 ± 100 Pas (T = 25 °C)
	10 ± 2 Pas (T = 25 °C)

	Thickness (MI 002)
	1100 ± 100 Pas (T = 25 °C)
	800 ± 100 Pas (T = 25 °C)
	/

	Color
	Different colours are available (e.g. straw, white, black, jura, dark jura etc.)

	Packaging
	
	
	

	STORAGE

	Keep the tins well sealed in a cool and ventilated place for a maximum of 12 months from date of production printed on the tin. 

	SAFETY RULES

	Ensure work area is well-ventilated during application and until surface is dry. It is recommended the use of personal protective equipment during application. Read the safety sheet before application.

	APPLICATION

	-  Make sure to thoroughly clean whatever surface areas you wish to bond together.
- Take from the tin the necessary amount of glue, using clean tools, and add 1 - 3 gr. of catalyst for 100 gr. of product;

-  Stir the two components energetically;

- Apply the mastic on the surface to be treated, taking into account that the mastic can be polished after about thirty minutes Applying the mastic at temperatures over 25 ° C will reduce curing time, conversely, lower temperatures will extend curing time;

- Do not return the unused catalyzed glue in the tin in order to avoid the entire content of the same deteriorates; 
- After use, close the tin in order to avoid hardening of the glue on contact with air.

	APPLICATION
	Spatula
	GEL TIME 
	2 – 6 min

	[image: image1.png]



	
	[image: image2.png]



	

	HARDENER 
	 dibezoyl peroxide 1 – 3 %
	DRY TO TOUCH (25 °C)
	5 - 20 min

	[image: image3.png]o+




	
	[image: image4.wmf]
	

	COMPLETE CURING (25 °C)
	 >20 min
	POLISHABLE (25 °C)
	After 30 min

 

	[image: image5.wmf]
	
	
[image: image6.wmf] 


	

	ADDITIONAL INFORMATION

	TYPE OF MASTIC
COLORS
VERSIONS
GEL TIME (min)
EXOTHERMIC PEAK
TIME (min)

T (°C)

TIXO

Different colors are available 

NORMAL
4 - 6
10 - 13
80 - 90
SEMISOLID
LIQUID
STRAW
HIGH SPEED
2
5
80 - 90
CATALYSIS (1 – 3 % of dibenzoyl peroxide) MI 003

	
[image: image7.wmf]TIME VS TEMPERATURE

0

10

20

30

40

50

60

70

80

90

100

0

1

2

3

4

5

6

7

8

9

TIME (MIN)

NORMALE

ACCELERATA


Catalysis (MI 003) is made with the 2% of dibenzoyl peroxide


ILPA ADESIVI SRL
Via Ferorelli, 4  –  Zona Industriale – 70123 BARI  – Italy  –  Tel. 0805383837 – Ass.  Tecnica  Tel. 0805308036 –  Export Dept. +390805308035 -  Fax +390805377807
Email:  ilpasrl@ilpa.it  –  http: // www.ilpa.it  –  Cap. Soc. € 218.400,00  i.v.  –  R.E.A. n. 152397  –  Cod. Fisc.  e   P. IVA  n. IT 00465900728  –  Reg. imp. Bari n. 6525

_1247463141.doc
[image: image1.png]






_1401004178.xls
Grafico1

		0		0

		2		2

		2.5		2.5

		3		3

		3.5		3.5

		4		4

		4.5		4.5

		5		5

		5.5

		6

		6.5

		7

		7.5

		8

		8.5



NORMALE

ACCELERATA

TIME (MIN)

TEMPERATURE (°C)

TIME VS TEMPERATURE

25

25

25.1

31.2

25.8

38.4

26.1

55

26.6

86.4

27.2

92.5

28.6

90.5

31.6

89.7

36.9

44.4

59.7

80.6

88

88.3

87.3



Foglio1

		NORMALE								SEMISOLIDO								ACCELERATA

		tempo		temperatura						tempo		temperatura						tempo		temperatura

		0		25						0		23.4						0		25

		2		25.1						2		24						2		31.2

		2.5		25.8						2.5		24.9						2.5		38.4

		3		26.1						3		25.6						3		55

		3.5		26.6						3.5		27.7						3.5		86.4

		4		27.2						4		30.7						4		92.5

		4.5		28.6						4.5		34.1						4.5		90.5

		5		31.6						5		39						5		89.7

		5.5		36.9						5.5		45.7

		6		44.4						6		50

		6.5		59.7						6.5		57.7

		7		80.6						7		65.5

		7.5		88						7.5		71.7

		8		88.3						8		77.7

		8.5		87.3						8.5		79.6

										9		81.7

										9.5		82.8

										10		83.4

										10.5		83.2

										11		82.8





Foglio2

		





Foglio3

		






